Strzeszczenie na konferencję

"Porous Glasses - Special Glasses - 2013 (PGL-2013)”

Politechnika Wroclawska 27 – 31.08.013

THE INVESTIGATION OF LOCAL STRUCTURE OF THE BORON AND LITHIUM IN SOME BORATE GLASSES BY MAS NMR SPECTROSCOPY

Bohdan V. Padlyak1,2*, Nikolay A. Sergeev3, Marcin Olszewski3,

Volodymyr T. Adamiv1, Yaroslav V. Burak1, Ihor M. Teslyuk1

1Sector of Spectroscopy, Institute of Physical Optics, Dragomanov Str. 23, 79-005 Lviv, Ukraine

2Division of Spectroscopy of Functional Materials, Institute of Physics, University of Zielona Góra,

Szafrana Str. 4a, 65-516 Zielona Góra, Poland

3Institute of Physics, University of Szczecin, Wielkopolska Str. 15, 70-451 Szczecin, Poland

The magic angle spinning nuclear magnetic resonance (MAS NMR) spectra of the 11B, and 7Li isotopes in a series of un-doped glassy and crystalline borate compounds with Li2B4O7, LiB3O5, LiCaBO3, LiKB4O7 and SrB4O7 chemical compositions were investigated and analysed. Investigated borate glasses of high optical quality and chemical purity were obtained from corresponding polycrystalline compounds using standard glass synthesis according to [1]. The borate single crystals were obtained by Czochralski method according to technological conditions, developed by authors.

The main structural units (BO3, BO4, and LiO4 atomic groups) and their proportions in the Li2B4O7, LiB3O5, LiCaBO3, LiKB4O7 and SrB4O7 glasses and polycrystals have been established based on the comparative analysis of the 11B and 7Li MAS NMR experimental spectra in them. The obtained results of MAS NMR spectroscopy show good correlation with X-ray diffraction data for local structure of the cationic sites in borate glasses [1] and crystals with same chemical compositions.

References

[1]	B.V. Padlyak, S.I. Mudry, Y.O. Kulyk, A. Drzewiecki, V.T. Adamiv, Y.V. Burak, I.M. Teslyuk, Mater. Sci.-Poland 30 (2012) 264.

# Footnotes

*Corresponding author. E-mail: B.Padlyak@proton.if.uz.zgora.pl. Fax: +48 (068) 328-2920.